## Slide 1
Progress Report Stuttgart
Dezember Meeting 2018
Stuttgart

## Slide 2
Source
ZBD
Wire Grid
Mirror
Faraday (45°)
Mirror
Mirror
Mirror
Sample +
Sample Holder
=
Optical Isolator
Measurement Setup
ZBD:
170 – 260 GHz
260 – 400 GHz
325 – 500 GHz (new)

## Slide 3
 Introducing an optical isolator into the signal path reduces the standing waves significantly and underlines as origin of the waves the path between source and detector. Half wavelength of the oscillations is approx. 1.2 m, which also fits to this distance between source and detector.
Here are presented pure transmission spectra without any signal processing (sample holder inside, no sample mounted):
Optical Isolator:
Effect of Optical Isolator

## Slide 4
Frequency Modulation:
Here are presented pure transmission spectra without any signal processing (sample holder inside, Sample 3, antennas not aligned with MW beam):
 Standing waves can be almost fully suppressed by frequency modulation of the MW beam.
 The following measurements are performed with 6 GHz FM, and little smoothing (Savitzky-Golay filtering) and no optical isolator.
Effect of Frequency Modulation

## Slide 5
 Broad resonance at a frequency of approx. 330 GHz
350 GHz antenna
 Higher g-value seems to increase absorption.
Comparison of Different g; 350 GHz

## Slide 6
350 GHz antenna
 Resonance vanishes at w = 0
Comparison of Different w; 350 GHz

## Slide 7
350 GHz antenna
319 GHz
342 GHz
366 GHz
Comparison of Different Steps; 350 GHz

## Slide 8
210 GHz antenna
 Maybe a small resonance around 300 GHz.
Resonances in Extended Range

## Slide 9
New Sample Holders
Automized (Stepper Motor)
Lock-in Amplification possible (Servo Motor)
Better Reproducibility
But still problems!

## Slide 10
Problems with Unexpected Signals
210 GHz Signal?
Unexpected Signals
Sample Holder:
Version 2
Modulation:
6 GHz
Isolator:
no
Sign of Resonance?
Sample:
New single antennas
210 GHz & 510 GHz

## Slide 11
Problems with Unexpected Signals
Sample Holder:
Version 2
Modulation:
6 GHz
Isolator:
no
Sample:
New single antennas
210 GHz & 510 GHz
210 GHz
Unexpected Signals still there. Not scaling whether an array or single antenna.
Sign of Resonance? Scaling with amount of antennas

## Slide 12
Problems with Unexpected Signals
Sample Holder:
Version 3
Modulation:
6 GHz
Isolator:
yes
Sample:
New single antennas
210 GHz
Background improved. Unexpected Signals still there
Sign of Resonance?

## Slide 13
Ideas for Improving Background Signal
Alignment of Center of the beam with rotation axis of the sample holder
Lock-in Amplification (Servo Motor)
Sample Holder material MW absorber (up to now Al)
???