## Slide 1: Progresses on Project
UNISTUTT
28. 1. 2021

## Slide 2
SPM LT measurement of calibration sample with Akiyama probe
Akiyama probe,
82 K at 1 bar He,
Nitrogen bath
Akiyama probe,
77 K at 1 bar He,
in cryostat
11. 8. 2020
7. 10. 2020
8. 10. 2020
Akiyama probe,
10 K at 1 bar He,
in cryostat
11. 11. 2020
Akiyama probe,
RT
outside cryostat
Height of squares is 120 nm
Akiyama probe

## Slide 3
Testing of TF probes with etched optical fiber tip on microscope LiteScope (NenoVision)
TF probe 1
TF probe 2
Height of squares is 20 nm
TF probe with etched optical fiber tip
Microscope LiteScope

## Slide 4
Sample
TF probe
Measurement of amplitude vs distance curves
Approaching
Approaching
SPM measurement of calibration sample with TF probes at RT
In nitrogen bath (84 K)
Height of squares is 120 nm
Height of squares is 120 nm
Classical AFM cantilever

## Slide 5
SPM unit
SPM probe + probe holder
Sample
Top sensor
Bottom sensor
Middle sensor
Installing and testing of NTC temperature sensors
Sample
TF probe
Nitrogen bath
Room temperature
Temperature response
in nitrogen bath
Top
Middle
Bottom

## Slide 6
Sample preparation in Brno – NiFe discs (fabricated by Peter Kepic)
10x10 mm undoped Si with 3x3 mm field of NiFe discs
10x10 mm quarz substrate with 3x3 mm field of NiFe discs
3x3mm undoped Si with 3x3 mm field of NiFe discs
3x3 mm quarz substrate with 3x3 mm field of NiFe discs
Samples:
for PETER setup
Reference for HFEPR setup
Discs thickness - 115 nm

## Slide 7
PETER laboratory
Bolometer
Microwave quasi-optics
Superconducting magnet, 0 - 12 T (Cryogenic Ltd.)
with cryostat enabling EPR measurements from 4 K to RT
PETER sample rod
with SPM unit
SPM unit
SPM probe + probe holder
Sample
Piezoscanner + stepping motors
Microwave waveguide
Coils for magnetic field modulation