## Slide 1: Fabrication of 5 mm disks from Permalloy and Copper phthalocyanines
PETER project
Peter Kepič, Jiří Liška, Tomáš Krajňák, Martin Konečný, Jan Čechal, Tomáš Šikola
Brno PETER meeting 2021/04/29

## Slide 2: Fabrication of Permalloy disks, film (done)
Fused silica
NiFe disk
Fused silica
NiFe
Fused silica
Fused silica
Resist
Fused silica
Substrate
cutting & cleaning
(Acetone, IPA, ultrasound)
Resist spincoating & EBL
CSAR AR-P6200.09
Developing
AR 600-564
+ IPA + DEMI
NiFe deposition
E-Beam Evaporator
Lift-off
Dioxolane for CSAR (AR 600-71)
Final sample (I.)
NiFe disks in central area 3x3 mm2
Diameter 5 mm, Pitch 80 mm
Height 90 nm
Fused silica substrate 10x10x0.5 mm3
Sample (II.)
Peter Kepič

## Slide 3: Fabrication of Copper phthalocyanines (CuPC) disks
Silicon
CuPC disk
Silicon
CuPC
Silicon
Silicon
Resist
Silicon
Substrate
cutting & cleaning
(Acetone, IPA, ultrasound)
Resist spincoating & EBL
CSAR AR-P6200.09
PMMA AR-P649.04
PMMA AR-P679.04
Developing
AR 600-564
AR 600-56
+ IPA + DEMI
CuPC deposition
MBE in UHV
(sample space limitation)
Lift-off
× Dioxolane for CSAR (AR 600-71),
CuPC destroyed quickly
OK Acetone for PMMA CuPC, destroyed slowly
Diameter 5 mm
Height ~100 nm
Pitch 10 mm
Expected sample
JL, Tomáš Krajňák, Peter Kepič

## Slide 4: Fabrication of Copper phthalocyanines (CuPC) disks
Silicon
CuPC disk
Silicon
CuPC
Silicon
Silicon
Resist
Silicon
Substrate
cutting & cleaning
(Acetone, IPA, ultrasound)
Resist spincoating & EBL
CSAR AR-P6200.09
PMMA AR-P649.04
PMMA AR-P679.04
Developing
AR 600-564
AR 600-56
+ IPA + DEMI
CuPC deposition
MBE in UHV
(sample space limitation)
Lift-off
× Dioxolane for CSAR (AR 600-71),
CuPC destroyed quickly
OK Acetone for PMMA CuPC, destroyed slowly
Diameter 5 mm
Height ~100 nm
Pitch 10 mm
Expected sample
JL, Tomáš Krajňák, Peter Kepič

## Slide 5: CuPC disks (optimization in progress)
Silicon substrate (3x3 mm2), PMMA AR-P 649.04, CuPC deposition (30 min), Lift-off using Acetone (10 s, ultrasound)
15-25 nm
CuPC disks stable in SEM
In-beam BSE (poor contrast)
Very faint CuPC disks present
in optical microscopy BF/DF
Silicon
CuPC disk
~15 nm
JL, Tomáš Krajňák, Peter Kepič

## Slide 6: CuPC disks (optimization in progress)
Silicon substrate (3x3 mm2), PMMA AR-P 649.04, CuPC deposition (15 min), Lift-off using Acetone (60 s)
6-8 nm
Silicon
CuPC disk
~7 nm
JL, Tomáš Krajňák, Peter Kepič

## Slide 7: Near future (close to finish)
Finishing fabrication 2 samples with appropriate thickness of CuPC film/disks (EBL done, CuPC deposition in progress – material refilled, pumping, new calibration, degassing)
Silicon or fused silica substrate is tested
CuPC film in central area 3x3 mm2
Thickness ~100 nm,
Si/Fused silica substrate 10x10x0.5 mm3
CuPC disks in central area 3x3 mm2
Diameter 5 mm, Pitch 10 mm
Height ~100 nm
Si/Fused silica substrate 10x10x0.5 mm3
Sample (III.)
Sample (IV.)
JL, Tomáš Krajňák, Peter Kepič