## Slide 1
AFM scanning parameters:
Scan field: 40 µm x 40 µm
Scan resolution: 512 x 512 points
Scan rate: 0.25 Hz (i.e. 20 µm/s)
Total scan time: cca 40 minutes
Environment: RT and in Air
Before scanning
After scanning (detail)
After scanning
Tip apex
Tip condition after single AFM scan of the calibration sample
Discs height: 120 nm

## Slide 2
PETER probe AFM test in cryostat at low temperature and in high magnetic field
Sweeping the magnetic field
10 T
10 - 6 T
6 - 1 T
6 T
In cryostat at 10 K (12 K)
In cryostat at 10 K (12K) and 12 T
In cryostat at 10 K (18K) and 12 T
Modulation at 2 KHz and 2 A (3G)