## Slide 1: Project PETER
Major topics: WP1 – Antennas/Probes
Nearest outcomes/tasks:
Planar plasmonic structures
USTUTT:
To measure antenna resonances on the sample available at Stuttgart for antennas with nominal resonances other than 210 MHz, i.e. 350 MHz and 490 MHz samples and the step (pitch) 2 (asap)
to explain the “wavy” character of the transmission spectra and, possibly, to improve them (asap)
CEITEC BUT:
a) F ≥ 1 THz
to fabricate and test (FT-IR) the samples for magnetic “hot” spot measurements (THz s-SNOM – R. Hillenbrand) – optimum frequency 2.5 THz (September 15)
to identify higher modes at simulations (asap) – LUMERICAL simulations (field distribution), (asap)
to interpret the appearance of additional peaks at smaller pitch (asap)
b) F ≤ 1 THz
fabrication of an additional sample with arrays of antennas tuned to more different nominal frequencies (smaller frequency steps) – better assignment of peaks to plasmon resonances (September 15)

## Slide 2: Project PETER
B. Scanning probes for PE THz EPR microscopy
NanoGune:
Fabrication of tips by FIB (starting: asap)
CEITEC BUT:
Exploring other potential ways of tip fabrication:
from optical fibres (starting: end of August)
by anisotropic chemical etching of Si – pyramids (September)
from sapphire shards (October – if the previous methods fail)
C. Tipped Enhanced EPR signal detection
NanoGune + CEITEC BUT:
To model and simulate a Plasmon-enhanced EPR signal (PE-EPR), (already has started)
how to separate the Plasmon-enhanced EPR signal from the background contribution (sample area external to the tip, primary beam reflected from the tip walls,….)? , (after successful simulation of the PE-EPR)

## Slide 3: Project PETER Optical fiber tip with a diabolo antenna
res = 120 m => 2,5 THz
L = 15 m
 (m)

## Slide 4
L = {14, 15, 16} m
L/2
FIB, angle {90°, 60°, 120°}
 100 m (Au)
Length of fiber 10 mm
90°
90°
L/2
90°
Conical tip
Pyramidal tip

## Slide 5
BSE
SE
SE
SE
BSE
2.
1.
3.
3.
3.
4.
BSE
Top view
Top view
Top view
Top view
Top view
Side view
50 m
18 m
9 m
FIB milling
of an optical fiber (with metal coating)
9 m
4.
Side view
BSE

## Slide 6
FIB milling of an optical fiber (without metal-coating)
Pyramidal tip

## Slide 7
FIBID (Pt precursor)
L = 4 m
Ellipsometry => complex refractive index
FTIR => resonance frequency
(250 x 450) m Pt antenna array on a Si substrate =>
250 m
450 m

## Slide 8: Project PETER
Summary of the present state:
WP1 – Antennas/Probes
Planar plasmonic structures
USTUTT:
There are the first promising results on measurement of resonant properties of antennas with fres < 1 THz
CEITEC BUT:
Additional antennas with fres < 1 THz have been fabricated and sent to USTUTT for measurements.
Antennas with fres = 2.5 THz have been fabricated and at present they are being tested by FT-IR for checking the resonant frequencies. They should be ready for handing over to Rainer in Brno.
B. Scanning probes for PE THz EPR microscopy
NanoGune :
Fabrication of tips by FIB – will be presented in Brno
CEITEC BUT:
An alternative method of tip fabrication from optical fibres has been tested. The achieved results are more than promising. Needs in Brno: the cantilevers used from NanoGune so that the tips can be attached to them - Rainer, will you please bring them to Brno?
C. Tipped Enhanced EPR signal detection
CEITEC BUT and NanoGune:
Modelling and simulation of the plasmon-enhanced EPR signal (PE-EPR) is in progress.

## Slide 9: Thank you

## Slide 10
substrate: FZ Si 100, resistivity 300 - 500 Wcm
Based on numerical simulations
Nine arrays of gold nanoantennas for FTIR experiments were designed and fabricated for three frequencies (1, 3, 10 THz) and three pitches (1.5, 2, 4 Dx/Dy)

## Slide 11
Relative reflectance spectra of three antenna arrays with pitch=1.5 (i.e. with highest density and therefore the largest signal). The plasmonic resonances are clearly visible, yet with a double-peak shape. We ascribe the appearance of double peaks to strong interaction between nanoantennas due to their close vicinity – for larger pitches (see below) double peaks dissapear and the resonances are red shifting towards their designed values.

## Slide 15
Here there are raw FTIR reflectance spectra (Bruker Vertex 80v) of the Au mirror (orange), reference Si substrate sample without antennas (grey), and 10 THz antenna array (red). Our samples show strong Fabry-Perot oscillations that we discard by low-pass FFT filtering (corresponding thick lines). Such filtered spectra of the antenna arrays are then divided by the filtered spectrum of the reference to get relative reflectance shown on slides below. Note that dividing by the Au mirror signal gives similar results (apart from small linear background) and that transmittance measurements (not shown) are fully complementary to these results.