## Slide 1: Progresses on Project
UNISTUTT
3rd of December 2020

## Slide 2: Progresses on Project
UNISTUTT
3rd of December 2020
P
X
E
E
T
R
I
M
E
N

## Slide 3
PETER laboratory
Bolometer
Microwave quasi-optics
Superconducting magnet, 0 - 12 T (Cryogenic Ltd.)
with cryostat enabling EPR measurements from 4 K to RT
PETER sample rod
with SPM unit
SPM unit
SPM probe + probe holder
Sample
Piezoscanner + stepping motors
Microwave waveguide
Coils for magnetic field modulation

## Slide 4
Testing of PETER setup (Alisa and Richard visit)
XY scan of cross-polar signal
Z scan of cross-polar signal
Alignment of microwave quasi-optics, heating test of the modulation coil
42°C after few min at 4 A and 2V – cca 10 G
Roof mirror
Detection and mapping of cross-polar signal – roof mirror mounted on SPM sample stage
(inside the cryostat)

## Slide 5
Measurement of Mn12ac (reference sample) on HFEPR setup – test sample for PETER setup
Mn12ac
Frequency: 350 GHz
Phys. Rev. B 56, 8192 (1997)

## Slide 6
Measurement of Mn12ac (reference sample) on HFEPR setup – test sample for PETER setup
Mn12ac
Frequency: 350 GHz
Phys. Rev. B 56, 8192 (1997)

## Slide 7
Measurement of Mn12ac (reference sample) on PETER setup
Frequency: 350 GHz
Phys. Rev. B 56, 8192 (1997)
HFEPR

## Slide 8
FDMR Measurement of Mn12ac (reference sample) on HFEPR setup – test sample for PETER setup
Stanford lock-in amplifier
Zurich Instruments lock-in amplifier
PCCP, 20, 15528 (2018)

## Slide 9
280 GHz
380 GHz
380 GHz
Time (s)
60 s
Magnetic field 1.1 T , Mod. Frequency 1.8 kHz, Mod. Amp 1 A, Temperature 10 K
EPR measurement in field domain:
Measured on PETER setup with
Stanford lock-in amplifier
FDMR Measurement of Mn12ac (reference sample) on PETER setup

## Slide 10: Progresses on Project
UNISTUTT
3rd of December 2020
S I M U L A T I O N S

## Slide 11
Array 3x3 - Gap sweep
SIMULATION 1:
Sweep 25 – 1000 um with steps 25 um
In-plane field averaged over this antenna

## Slide 12
Array 3x3 – Antennas gap sweep

## Slide 13
Array 3x3 - Gap sweep

## Slide 14
Array 3x3 - Gap sweep – Analysis of Plasmonic modes

## Slide 15
According to the analysis of Acuna et al., we calculate at which frequency we can expect a plasmonic mode
G = 2*pi/a
In our case:
a = 248+120 um = 368 um
Therefore G = 170 cm-1
And according to this, the plasmon mode should be at ca. 380 GHz.
Array 3x3 - Gap sweep – Analysis of Plasmonic modes

## Slide 16
Array 3x3 – Substrate lateral size sweep
direct
inverse

## Slide 17
Array 7x7 – Substrate thickness sweep

## Slide 18
Array 7x7 – Substrate thickness sweep

## Slide 19
Array 7x7 – Substrate thickness sweep
Red lines are given by:

## Slide 20
Array 7x7 – Substrate thickness sweep
Red lines are given by:
More from Martin H.